## Slide 1: Effectiveness Factors for Electrochemical Reactions in SOFC Electrodes
Jin Hyun Nam, Ph. D.
School of Mechanical Engineering
Daegu University
Notes: Thank you, Dr. Beal.
Hello.
Today, I will talk about the effectiveness factors for electrochemical reactions in electrodes of solid oxide fuel cells.

## Slide 2: Electrode Process
Fuel cell process
  Electronic and ionic charge conduction
  Distributed electrochemical reactions
  Gas species transport (+ heat transfer)
Electrode micro model
  Charge conservation
  Nonlinear electrochemical reaction
  Gas species conservation (+ energy conservation)`
Volumetric exchange current density (A/m3)
Activation
overpotential (V)
(Butler-Volmer eq.)
Volumetric charge transfer current density (A/m3)
Anode process
Notes: Let me start with the electrode process in SOFCs.
The fuel cell process in the electrode involves electronic and ionic charge conduction, distributed electrochemical reaction, and gas species transport. And also heat transfer is involved.
This complex process has been solved by the so-called electrode micro models. The micro models fully consider the electronic and ionic charge conservation, nonlinear reaction kinetics, and gas species and energy conservation in the electrode.
This is Butler-Volmer equation which is widely used to model the relationship between the charge transfer current and local activation overpotential. And this is the exchange current density.

## Slide 3: Pros and Cons of Electrode Micro Model
Advantages
  Accurate prediction of the current generation vs. overpotential (i) performance of electrodes
  Detailed investigation of the electrode process, including the effects of microstructural parameters on performance
  Thus, most suitable for theoretical research of complex electrode structures (FGEs, MGEs) and their performances
Disadvantages
  High computational costs: many variables on grid points
  (e.g. at least 20 highly non-uniform grid points in 20-m-thick reaction layers)
  Difficult to be employed in CFD simulation codes
Electrode effectiveness model, which enable
  Accurate and efficient prediction of the i performance
  Full consideration of the effects of microstructural parameters
Notes: The advantages of the electrode micro model includes the accuracy of results, and the detailed investigation of the fuel cell process and microstructural effects. Thus, the electrode micro models are considered as the most suitable model for theoretical research of complex electrode structures, including functionally-graded or structurally-graded electrodes.
However, the micro model generally requires too much computational costs because many variables should be considered with many grid points. This makes it difficult to employ the micro model in CFD simulations.
Thus, we attempted to develop an effectiveness model, to easily and accurate predict the current generation in the electrode while fully considering the microstructural effects.

## Slide 4: Simplifying Assumptions
Active reaction layers
  Dedicated reaction layers in multi-layer electrode structures
  Formed near the electrolyte, thin (~20 m), dense (~25% porosity), and fine particle size (high TPBL density ~51012 m/m3)
  Current generation is completed in the active reaction layer
Practical assumptions
  Homogeneous microstructure  the volume-specific TPB length (TPBL), tpb,V, and effective ionic conductivity, io,eff, are uniform
  Sufficiently thin layer thickness  Uniform operating condition (T, pt, xi)  the TPBL-specific exchange current density, itpb, Nernst potential, o, and concentration overpotential, conc, are uniform
  High effective electronic conductivity  the electronic potential, el, is uniform
Focus of this study
Notes: To develop the effectiveness model, we focused on the active reaction layer, which is a dedicated layer for electrochemical reactions in multi-layer electrode structures.
This layer is thin, dense, and formed directly on top of the electrolyte, and has fine particle size to increase three-phase boundary length (TPBL). In general, the current generation is almost completed inside the active reaction layer.
Also these layers are called as the anode functional layer (AFL) or cathode functional layer (CFL).
We take the following practical assumptions to simplify the model equations, that is, homogeneous microstructure, sufficiently thin layer thickness, and high effective conductivity.
With these assumptions, volume-specific TPBL, effective ionic conductivity, TPBL-specific exchange current density, Nernst potential, concentration overpotential, and electronic potential, all of these are uniform inside the active reaction layer.

## Slide 5: Simplified Model Eq. : Anode Reaction Layer
Ionic charge conservation
Electrochemical reaction
Activation overpotential
: Volumetric exchange current density (A/m3)
and
These are constant in the layer
Total activation overpotential applied to
the layer
()
*These equations are also valid for cathode!
*also called as anode functional layer (AFL)
(†)
(†)
Notes: The current transport in the active reaction layer of an anode is shown in this figure, where electronic current is transported, converted into ionic current by the transfer current.
In the simplified model, ionic charge conservation is expressed in terms of activation overpotential, eta, and the electrochemical reaction is expressed by Butler-Volmer equation. Here, this terms is equivalent to volumetric exchange current density.
And the local activation overpotential is expressed as follows, where electronic potential, Nernst potential, and concentration overpotential are constant in the active reaction layer.
In the boundary conditions, the total activation overpotential is defined as follows.

## Slide 6: Effectiveness Factor: Linear Reaction Kinetic
Definition of eff
  Ratio of actual electrochemical reaction rate to maximum rate
  Reaction rate ~ current generation rate (current density)
  Maximum rate is obtained when all TPBs in the active reaction layer (0zL) are subject to tot (in reality, tot, thus, 0eff1)
Linear charge transfer reaction
  For itr,V() follows
Active
layer
thickness
(m)
(Costamagna et al., 1998)
where
Electrochemical Thiele modulus
Exact solution
(A/m2)
Notes: Then, the effectiveness factor is defined as the ratio of actual electrochemical reaction rate to maximum rate, as follows. Note that the reaction rate is equivalent to current generation rate, or current density.
Here, the maximum current generation is obtained when all three-phase boundary sites in the active reaction layer are subject to total activation overpotential. In fact, local activation overpotential is always smaller than total overpotential, effectiveness factor falls between 0 and 1.
Costamagna et al. considered the problem when charge transfer reaction is described by linear equation as follows, and obtained the following exact solution. This is the effectiveness factor and this is Thiele modulus.

## Slide 7: Effectiveness: Nonlinear Reaction Kinetic
Nonlinear Butler-Volmer reaction
  Effectiveness factor can be decomposed into two parts:
  eff,0V: Base effectiveness at zero overpotential (0)
  : Relative effectiveness at finite overpotential
Determination of
  Numerically solved the simplified model equations()
  Finite difference method (FDM) with 2000 uniform grid points
  eff is calculated, and divided by eff,0V to obtain
(Shin and Nam, 2015)
Dimensionless
total activation
overpotential
Notes: For nonlinear reaction kinetics, such as Butler-Volmer equation, Shin and Nam showed that the effectiveness factor can be decomposed into two parts. These are the base effectiveness at zero overpotential, which is the same as the effectiveness factor for linear systems, and the relative effectiveness at non-zero overpotentials.
The relative overpotential is a function of both Thiele modulus and dimensionless total activation overpotential defined as follows.
Extensive numerical calculations were done to determine the relative effectiveness factors, and

## Slide 8: Relative Effectiveness Data (=0.5)
Symmetric
Butler-Volmer Eq.
Behaviors of f(tot)
  Function of Thiele modulus, T, and dimensionless
  For very small T, f  1.0, irrespective of
  For moderate T, f decreases from 1.0 to 0.0 as increases
  For T3, f has a converged functional shape, irrespective of T
At T=1000 K (=0.5),
tot=00.3 V in the anode
corresponds to
and in the cathode
to
~
Notes: This is the obtained relative effectiveness factors for symmetric Butler-Volmer reaction kinetics with alpha equals 0.5.
At a given Thiele modulus, the relative effectiveness decreases from 1 towards 0 as the dimensionless total overpotential increases. And the relative effectiveness approaches to 1 when Thiele modulus is very small. It is interesting that the shape of the relative effectiveness does not change when Thiele modulus is higher than 3.
Please note the range of the dimensionless total activation overpotential for anode and cathode.
In the figure, the symbols denote the numerically obtained data while the lines denotes the correlation equations, which is defined as

## Slide 9: Relative Effectiveness Correlation (=0.5)
Correlation Eq.
  Linear interpolation of coefficients is required for T not listed
  Estimated error is less than 0.8% (for cathode total overpotential range of tot=00.4 V at 1000 K)
T | a | b | c | d | Err0.3V | Err0.4V
4 | 1.1199 | 0.7876 | 1.1332 | 0.3922 | 0.7% | 0.7%
3 | 1.1208 | 0.7925 | 1.1392 | 0.3946 | 0.7% | 0.7%
2.5 | 1.1241 | 0.8060 | 1.1504 | 0.4013 | 0.7% | 0.7%
2 | 1.1286 | 0.8333 | 1.1858 | 0.4148 | 0.7% | 0.7%
1.8 | 1.1318 | 0.8540 | 1.2152 | 0.4250 | 0.8% | 0.8%
1.6 | 1.1337 | 0.8789 | 1.2631 | 0.4372 | 0.8% | 0.8%
1.4 | 1.1337 | 0.9098 | 1.3394 | 0.4522 | 0.8% | 0.8%
1.2 | 1.1336 | 0.9564 | 1.4624 | 0.4756 | 0.8% | 0.8%
1 | 1.1245 | 1.0010 | 1.6579 | 0.4976 | 0.8% | 0.8%
0.8 | 1.1068 | 1.0469 | 1.9636 | 0.5203 | 0.7% | 0.7%
0.7 | 1.0944 | 1.0684 | 2.1755 | 0.5310 | 0.7% | 0.7%
0.6 | 1.0798 | 1.0864 | 2.4384 | 0.5399 | 0.6% | 0.6%
0.5 | 1.0634 | 1.1002 | 2.7681 | 0.5464 | 0.6% | 0.6%
0.4 | 1.0467 | 1.1089 | 3.1882 | 0.5503 | 0.5% | 0.5%
0.3 | 1.0304 | 1.1107 | 3.7422 | 0.5500 | 0.4% | 0.4%
0.2 | 1.0162 | 1.1030 | 4.5285 | 0.5433 | 0.3% | 0.4%
0.15 | 1.0102 | 1.0944 | 5.0856 | 0.5363 | 0.3% | 0.4%
0.1 | 1.0053 | 1.0783 | 5.8603 | 0.5224 | 0.2% | 0.3%
0.07 | 1.0028 | 1.0621 | 6.5305 | 0.5069 | 0.2% | 0.3%
0.05 | 1.0016 | 1.0479 | 7.1565 | 0.4910 | 0.1% | 0.1%
Notes: The proposed correlation equation is expressed like this and the correlation coefficients are tabulated like this. The estimated error between the numerically determined effectiveness data and estimated effectiveness by correlation is always smaller than 0.8%.
Thus, the correlation equation and coefficients can be used to easily and accurately retrieve the effectiveness data.

## Slide 10: Using Electrochemical Effectiveness
Calculation steps
  For given conditions in the active reaction layer:
  Calculate the TPBL-specific exchange current density, itpb, or the TPBL-specific polarization resistance, rtpb
  Calculate the electrochemical Thiele modulus, T
  Calculate the base effectiveness, eff,0V, and the relative effectiveness, f(tot), and the effectiveness factor, eff
  Finally, calculate the current density, ireal,A, as follows:
Total activation
overpotential
Active layer
thickness
Base
effectiveness
Relative
effectiveness
TPBL-specific
polarization resistance
~
Notes: Now, how to use the obtained effectiveness factor is explained as follows.
First, for a given uniform operating condition in the active reaction layer, calculate the TPBL-specific exchange current density or TPBL-specific polarization resistance. Then, this is used to determine Thiele modulus.
Then, the base effectiveness and relative effectiveness are calculated and multiplied to determine the effectiveness factor
Finally, the total current density generated in the active reaction layer is calculated, in the unit of Ampere per square m, as follows

## Slide 11: Model Validation: Electrode Performance
Microscale vs. effectiveness model: Comp. of i-tot curves
  Uniform T and pi conditions
  Microscale model results are obtained by using 400 grid points
  Effectiveness model results are determined as explained
  General range of T is about 520 for AFLs and 0.52.5 for CFLs
Notes: The validity of the effectiveness model is demonstrated by comparing the electrode micro model results, denoted by the symbols, and the effectiveness model results, denoted by the lines. Isothermal and isoconcentration conditions are assumed for calculation.
Here, the electrode micro model results were obtained by solving the detailed charge conduction and electrochemical reaction with 400 grid points placed in 20-micrometer-thick anode functional layers or cathode functional layers. The effectiveness model results were calculated using spreadsheet software as expressed previously.
Almost perfect agreements are observed, and this clearly indicates the validity of the effectiveness model.
One thing to note is that the range of Thiele modulus encountered in the ordinary operation of IT-SOFCs. Thiele modulus generally falls between 5 and 20 for anode functional layers and 0.5 and 2.5 for cathode functional layers.

## Slide 12: Model Validation: 1D Cell Performance
Comparison of
  Experiential performance of single-cell IT-SOFC
  Comprehensive micro model results
  Effectiveness-based micro simulation results
20 Volume cells are placed
in AFL & CFL for comprehensive
Micro model, while only 2 cells
are placed for effectiveness-
based model
(Zhao and Virkar, 2005)
(Jeon et al., 2006)
*Isothermal but gas species transport are considered
(Shin et al., 2016)
Notes: In addition, one-dimensional single-cell performance of IT-SOFCs was simulated using the effectiveness-based simulation model, and the results were compared with the comprehensive microscale model simulation results. In this case, isothermal condition is assumed but gas species transport in the anode and cathode was fully considered.
As shown in this figure, very good agreements are also obtained, although only small numbers of grid points are placed in the anode functional layer and cathode functional layer for the effectiveness-based simulation model.

## Slide 13: Asymptotic Behaviors
Effectiveness behavior
  As T0.05, tanh(T)/T  1 & f  1
  For T3, tanh(T) )/T  1/T & the shape of f does not change
Low modulus (T0.05)
High modulus (T3)
Microstructural Effects
This has a fixed function shape
  *anode reaction layer generally falls in this range
  Volume-specific TPBL
  Effective ionic conductivity
  Active reaction layer thickness
Notes: Now, let’s look into the asymptotic behaviors of the effectiveness factor. For very small Thiele modulus, both the base effectiveness and relative effectiveness approaches to 1. For Thiele modulus higher than 3, the base effectiveness becomes one over Thiele modulus and the functional shape of relative effectiveness does not change.
Then, the asymptotic behaviors for total current generation can be expressed as follows. For low modulus conditions, total current density is directly proportional to the volume-specific TPBL and active layer thickness.
And for high modulus, total current density is proportional to the square of the volume-specific TPBL and effective ionic conductivity, but not dependent on the layer thickness.

## Slide 14: Numerical Experiments of Degradation
Degradation of tpb,V and io,eff is simulated (upto 9% reduction)
  Guiding lines are drawn by only scaling the undegraded (100%) performance curves
AFL
AFL
CFL
CFL
Degradation results are obtained by the electrode microscale simulations with 400 grid points in AFL or CFL
For AFL, the relations
show almost perfect agreement.
For CFL, the relations show some disagreement.
(Baek et al., 2016)
Notes: Numerical experiments are conducted to investigate the effects of the microstructural degradation, where the volume-specific TPBL and effective ionic conductivity is reduced up to 9% of the original values.
In the figure, the degradation results were obtained by detailed electrode micro model by placing 400 grid points in the anode functional layers and cathode functional layers. Also, the guiding lines shown in the figure were obtained by only scaling the undegraded (100%) performance curves.
In the figure for the anode functional layer, total current density perfectly follows the relationship that total current density is proportional to the square of the volume-specific TPBL and effective ionic conductivity. Please recall that Thiele modulus generally falls between 5 and 20 for anode functional layers.
The performance curves for the cathode functional layer show some small disagreements with the relationship.

## Slide 15: Sensitivity Map for Symmetric BV Eq. (=0.5)
Effects of microstructural parameters on current generation
  Dependence exponents are equivalent to sensitivities
  TPBL exponent, m:
  Ionic cond. exponent, m:
  Thickness exponent, mL:
For small T, m’s converge to
m, m, mL  1, 0, 1
For moderate T, m’s depend on
both T and tot
~
For T3, m’s converge to
m, m, mL  0.5, 0.5, 0
Notes: Finally, a complete sensitivity map was devised to predict the effects of volume-specific TPBL, effective ionic conductivity, and active layer thickness on the current generation in AFL and CFL. Note that the dependence exponents are equivalent to variable sensitivities.
For small Thiele modulus, the TPBL exponent, ionic conductivity exponent, and thickness exponent converge to 1, 0, and 1, respectively. For moderate Thiele modulus, the dependence exponents are functions of Thiele modulus and dimensionless total activation overpotential. For Thiele modulus larger than 3, the TPBL exponent, ionic conductivity exponent, and thickness exponent converge to 0.5, 0.5, and 0, respectively

## Slide 16: Conclusion
An electrochemical effectiveness model is proposed based on some practical assumptions, which
  Enables easy determination of current generated in thin active reaction layers (AFL, CFL) without resorting to complex microscale electrode models
  Is still capable of accurately considering the effects of electrode microstructural parameters on current density
  Can be readily incorporated with CFD simulation codes because only small numbers of grid points are required in the active reaction layers
A theoretical model is also proposed to based on the effectiveness model, to explain
  the effects of microstructural parameters on current generation performance in thin active reaction layers
Notes: The conclusion of this study is as follows.
An electrochemical effectiveness model is proposed, and this model enables efficient calculation of current generation in the active reaction layers and full consideration of microstructural effects. Thus, the effectiveness model is expected to be readily incorporated with CFD simulation codes.
In addition, a theoretical model is proposed to explain the effects of microstructural parameters on the current density generated in the active reaction layers.

## Slide 17: Thank you for your attention.
Notes: And thank you for your attention.