## Slide 1
Research Background & Objectives
Conventional electrode microscale models are difficult to be incorporated with large-scale macroscale calculations and computational fluid dynamics (CFD)
  Too many grid points are required for capturing the reaction/transport process in mixed ionic-electronic conducting (MIEC) electrodes
  Computational costs are also high due to this fine grid allocation
 Research Background
 Objectives
Development of an efficient and accurate method to determine the current generation in thin active reaction layers
Using the fewest grid points to speed up computation
Contact information
* Corresponding author. jinhnam@gmail.com (J.H. Nam).
Conclusion
An electrochemical effectiveness model is developed for efficient determination of current generated in active reaction layers of solid oxide fuel cells (SOFCs)
The accuracy of the electrochemical effectiveness model is validated
A theoretical prediction model is also proposed for the effects of microstructural parameter variation on the current generation performance
Theory and Calculations
Fig. 1 Electrochemical reaction/ charge transport process in anode functional layer
 Active Reaction Layer
Also called the active functional layer
Located just adjacent to the electrolyte, where most electrochemical reactions occur
Made of fine electronic & ionic particles to provide large three-phase boundaries (TPBs)
Usually made very thin (10-20 µm) and dense (porosity ~0.25) for multi-layer electrodes
 Basic Assumptions (Ideal Process)
The operating condition inside the active reaction layer is uniform due to small thickness (Uniform temperature, pressure, species concentration)
Electron conduction is fast due to high electronic conductivity (Uniform electronic potential)
Symmetric Butler-Volmer reaction kinetics at TPBs
For AFL, overpotential  is defined:
Charge conservation
Boundary conditions
Effectiveness factor
Main parameters
k = 1 for anodic, 2 for cathodic reaction
 Governing Equations for Reaction/Transport Problem
Electrochemical Effectiveness Model
Fig. 2 Relative effectiveness factors:
Data and correlation curves
 Effectiveness Data
The governing equation is solved with 2000 uniform grid points for various conditions
The obtained effectiveness factor is decomposed and summarized as follows
Total current generated in active react. layer(★)
Effectiveness factor
decomposition
Thiele modulus
Base effectiveness at zero overpotential
Relative effectiveness at finite overpotential
Dimensionless overpotential
 Relative Effectiveness
The relative effectiveness decreases from 1.0 towards 0.0 with overpotential
For T>3, the relative effectiveness converges into a single functional curve
A simple correlation equation is devised to retrieve the relative effectiveness
Less than 1% error
at normal conditions
T | a | b | c | d
4 | 1.1199 | 0.7876 | 1.1332 | 0.3922
3 | 1.1208 | 0.7925 | 1.1392 | 0.3946
2.5 | 1.1241 | 0.8060 | 1.1504 | 0.4013
2 | 1.1286 | 0.8333 | 1.1858 | 0.4148
1.8 | 1.1318 | 0.8540 | 1.2152 | 0.4250
1.6 | 1.1337 | 0.8789 | 1.2631 | 0.4372
1.4 | 1.1337 | 0.9098 | 1.3394 | 0.4522
1.2 | 1.1336 | 0.9564 | 1.4624 | 0.4756
1 | 1.1245 | 1.0010 | 1.6579 | 0.4976
0.8 | 1.1068 | 1.0469 | 1.9636 | 0.5203
0.7 | 1.0944 | 1.0684 | 2.1755 | 0.5310
0.6 | 1.0798 | 1.0864 | 2.4384 | 0.5399
0.5 | 1.0634 | 1.1002 | 2.7681 | 0.5464
0.4 | 1.0467 | 1.1089 | 3.1882 | 0.5503
0.3 | 1.0304 | 1.1107 | 3.7422 | 0.5500
0.2 | 1.0162 | 1.1030 | 4.5285 | 0.5433
0.15 | 1.0102 | 1.0944 | 5.0856 | 0.5363
0.1 | 1.0053 | 1.0783 | 5.8603 | 0.5224
0.07 | 1.0028 | 1.0621 | 6.5305 | 0.5069
0.05 | 1.0016 | 1.0479 | 7.1565 | 0.4910
 Validation
Compared the predicted current generation in active reaction layer
Effectiveness model results were obtained simply using Eq. (★)
Electrode microscale model results were obtained with 400 grid points in the layer
Good agreement is obtained, ensuring the accuracy of the effectiveness model
Fig. 3 Comparison of total current generation in active reaction layers,
predicted by the effectiveness model and electrode microscale model
An Effectiveness Model for Predicting
The Electrochemical Performance of SOFC Electrodes
Jin Hyun Nam1,*, Dongwoo Shin2
1School of Mechanical & Automotive Engineering, Daegu University, KOREA
2School of Mechanical & Aerospace Engineering, Seoul National University, KOREA
Prediction Model for Electrode Microstructure Variation
 Peculiar Behavior of Relative Effectiveness
As T  0, the relative effectiveness approaches 1.0
For T>3, the shape of the relative effectiveness does not change
These behavior leads to the following asymptotic relationship
Low modulus (T 0.05)
High modulus (T  3)
 Total Current Generation in Active Reaction Layer
Table 1 Dependency of total current generation in active reaction layer on microstructural parameters
 Numerical Experiment: Microstructural Degradation
Degradations of volume-specific TPBL and effective ionic conductivity were simulated
Guiding lines drawn by only scaling the undegraded (100%) performance curves
Fig. 4 Anode degradation simulation results
Fig. 5 Cathode degradation simulation results
Current generation in the anode is nicely predicted by
That in the cathode is relatively well predicted, especially at high overpotential
Further studies are under way to determine the dependence for 0.05<T<3
Higher overpotential range (0-0.4 V)
() irrespective of overpotential
()
()