## Slide 1
Research Background & Objectives
A microscale model for intermediate-temperature SOFCs (IT-SOFCs) is required, which can consider simultaneous electrochemical oxidation of H2 and CO with
  Detailed consideration of the electrochemical reactions and charge/mass transport processes in the electrodes
  Experimentally-determined polarization resistance for each electrochemical reactions in three-phase boundaries (TPBs) of the electrodes
 Research Background
 Objectives
Development of a one-dimensional microscale model for IT-SOFCs considering simultaneous H2/CO co-oxidation in TPBs of the anodes
Using the developed model, the H2/CO co-oxidation characteristics during the operation of IT-SOFCs are studied
Contact information
* Corresponding author. jinhnam@gmail.com (J.H. Nam).
Conclusion
A microscale model for IT-SOFCs is developed to investigate H2/CO co-oxidation characteristics inside the Ni/YSZ cermet anodes
Numerical errors in single-cell performance due to different modeling approaches are quantitatively analyzed for model H2/H2O/CO/CO2 mixture gas and methane reformate
The H2 oxidation model with WGS reaction is found to predict the performance of IT-SOFCs with steam/methane reformate gas with less than ~10% error
Numerical Model Validation
 Single-cell IT-SOFC Performance from Zhao & Virkar JPS (2005)
Anode-supported IT-SOFC with 5 layer structure
Microscale Model Development for Intermediate Temperature
Solid Oxide Fuel Cells considering H2/CO Co-oxidation
Jaeyeong Song1, Areum Jeong1, Jin Hyun Nam2,*, Charn-Jung Kim1
1 Sch. of Mechanical & Aerospace. Eng., Seoul Nat’l Univ., Seoul 08826, Republic of Korea
2 Sch. of Mechanical Eng., Daegu Univ., Gyungsan 38453, Republic of Korea
Results and Discussion
 Performance with Methane Reformate
Fully-reformed CH4/H2O mixture fuel gas
@ 1 bar, 800C, S/C=2.0, 2.5, 3.0
Quantitative analysis for error from ignoring CO co-oxidation
For H2-rich condition, error is rather small (~1%)
As H2 concentration decreases, the contribution of CO oxidation to current generation increases
Error is estimated ~4% when 50% H2 is consumed and ~10% when 80% H2 is consumed
(a)
(b)
(c)
(a)
(b)
(c)
 Performance with H2/H2O/CO/CO2 Gas
Model fuel gas composition is considered
Errors with different model approaches are quantitatively analyzed
When H2/H2O concentration is high, different modeling approaches produce similar performance curves
As CO/CO2 concentration increases, H2/CO co-oxidation model is desirable
Considering WGS reaction generally improves the solution accuracy with H2 oxidation model
 Binary Fuel Gas: H2/H2O & CO/CO2
Effects of binary fuel composition on single-cell performance is studied
Similar performance trend is found in experimental results by Jiang & Virkar JES (2003)
Limiting current density is much smaller for CO/CO2 system; which is due to higher diffusion resistance of CO/CO2 compared with H2/H2O system
Theory and Calculations
 Basic Assumptions
Anode-supported IT-SOFCs with five-layer PEN structure 
Electrochemical reaction occurs only in thin functional layers, i.e., anode functional layer (AFL) and cathode (CFL)
Functional layers (AFL, CFL) are made of fine electronic/ionic particles, and thus have large TPB length
Bulk layers (ASL, CCCL) provides the path for electronic conduction and mass diffusion
Electronic charge conservation
Volumetric transfer current (A/m3)
 Governing Equations
Ionic charge conservation
Gas species conservation
Volumetric species source (mol/m3)
Maxwell-Stefan
equation
Ohm’s law
Boundary Conditions
 Volumetric Transfer Current
Volumetric-specific TPBL (m/m3)
H2 oxidation on Ni/YSZ TPBs
Bieberle et al. JES (2001)
TPBL-specific resistance
Overpotential
( m)
H2 + O2-  H2O + 2e-
CO oxidation on Ni/YSZ TPBs
Utz et al. JPS (2011)
TPBL-specific resistance
Overpotential
CO + O2-  CO2 + 2e-
O2 reduction on LSM/YSZ TPBs
Radhakrishnan et al. JES (2005)
TPBL-specific resistance
Overpotential
( m)
O2 + 4e-  2O2-
Intrinsic reaction kinetic
 Water-Gas Shift (WGS) Reaction and species sources
CO + H2O  CO2 +H2
(mol/m2cat-s)
Xu and Froment AIChE J (1989)
WGS species sources
(mol/m3-s)
Volume-specific Ni surface area (m2cat/m3)
Electrochemical species sources
Very good agreements are obtained, which indicates the validity of the present model
Microstructural parameters are provided, except mean particle diameter ( assumed)
Layer | Thickness | Porosity | Electronic phase fraction | Particle diameter()
ASL | 1000 μm | 0.48 | 0.55 | 1 μm
AFL | 20 μm | 0.23 | 0.55 | 0.5 μm
ELEC | 8 μm | − | − | −
CFL | 20 μm | 0.26 | 0.475 | 0.5 μm
CCCL | 50 μm | 0.45 | 1.0 | 1 μm
Operating @ 1 bar & xH2=0.97, xO2=0.21